2.5L SOFT STRETCH | 2.5-layer fabric, soft jersey-surface that lends the fabric high elasticity. The membrane on the reverse side has a functional printed texture, which

keeps the fabric from sticking to the skin. The material is light, stretchy and highly breathable.

Composition: 100 % Polyester Weight: 77 g/m2

Washing Instructions: 40 °C Breathability (g/m2 / 24 h): 20,000 Water Column (mm): 20,000

2.5 L МЯГКИЙ СТРЕТЧ | Ткань из 2.5 слоёв. Верхний слой из мягкого джерси, который придает ткани высокую эластичность. На внутренней стороне имеется мембрана с функциональной принтованной текстурой, которая не позволяет ткани скользить по коже. Материал легок, эластичен и очень воздухопроницаем.

Состав: 100% Полиэстер

Вес: 77 г/м²

Рекомендации по стирке: Стирать при 40°C

Воздухопроницаемость (г/м²/24 ч): 20,000

Давление в водной колонке (мм): 20,000